**CATALYTIC PERFORMANCE AND COKING RESISTANCE OF MODIFIED Ni/GDC ELECTRO-CATALYSTS FOR BIOGAS FUELED SOFCs**

**E. Ioannidou1\*, F. Zaravelis1,2, Α. Tatakis1,2, A. Souvalioti1,2, S. Neophytides1\*, D. K. Niakolas1\***

1 Foundation for Research and Technology, Institute of Chemical Engineering Sciences (FORTH/ICEHT), Stadiou Str., 26504 Platani, Patras

2Department of Chemical Engineering, University of Patras, 56504

*\***eioannidou@iceht.forth.gr**,* *neoph@iceht.forth.gr*, *niakolas@iceht.forth.gr*

**ABSTRACT**

Recycling biogas to produce syngas (H2 + CO) through Dry Reforming of Methane (DRM) has currently attract resurgent interest. Biogas consists mainly of CH4 (50-70%) and CO2 (25-50%) and is widely produced by anaerobic fermentation of biomass [1]. DRM provides a feasible solution to eliminate greenhouse gases via production of useful chemicals and hydrocarbons.

Considering the DRM energy applications the produced syngas can be used as a fuel in high temperature solid oxide fuel cells (SOFCs) for electricity production or biogas can be directly fueled in the cell without the need of an external reformer (Internal Dry Reforming of Methane, IDRM), which simplifies the SOFC system and reduces the cost [2,3]. Specifically, during IDRM at temperatures higher than 800 oC, the catalytic Reverse Water Gas Shift (RWGS) reaction may run in parallel with electrocatalytic reactions, resulting in the consumption of valuable H2. In addition, carbon deposition on the electrocatalyst surface due to CH4 decomposition, which is favored at elevated temperatures (≥ 700 oC), may also occur resulting in progressive electrocatalyst deactivation [4].

Ni-based ceramic-metal composites with Yttria Stabilized Zirconia (YSZ) and Gadolinia Doped Ceria (GDC) are widely used as electrocatalysts in SOFCs because of their activity and inexpensiveness. However, nickel catalyses the formation of carbon deposits from hydrocarbons and exhibits a tendency to agglomerate after prolonged operation [3,4]. The carbon tolerance and anti-sintering tendency of nickel and specifically of Ni/GDC can be enhanced, by dispersing trace amounts of transition noble (Rh, Pt, Pd, Ru, Au) or non-noble (Co, Cu, Mo, Fe) metal elements [3,5].

In this study the performance of Ni/GDC, 1 wt.% Au-Ni/GDC, 3 wt.% Au-Ni/GDC, 0.5 wt.% Fe-Ni/GDC, 2 wt.% Fe-Ni/GDC, 3 wt.% Au-3 wt.% Mo-Ni/GDC and 3 wt.% Au-0.5 wt.% Fe-Ni/GDC electrodes have been studied, at open-cirquit potential conditions, under biogas fuel operation in single SOFCs. The electrodes have been tested in the form of half-electrolyte supported cells, at 750-900 oC, under a fuel with a ratio of CH4 to CO2 equal to 1 and for total gas flows varying from 150 to 300 cc/min. The catalytic kinetic measurements were carried out under differential conditions, at various CH4 and CO2 partial pressures. In addition, the catalytic CH4 dissociation reaction at 800 oC and other physicochemical properties of the powders were examined via TGA, XRD and H2-TPR.

**KEYWORDS:** Solid Oxide Fuel Cells (SOFCs), Dry Reforming of Methane (DRM), Biogas, Ni-based electrodes, Open Cirquit Conditions

**REFERENCES**

[1] Escudero, M.J., Maffiotte, C.A. & Serrano J.L. (2021). *J. Power Sources.* 481 (20) 229048.

[2] Souentie, S., Athanasiou M., Niakolas, D.K., Katsaounis, A., Neophytides, S.G. & Vayenas, C.G. (2013). *J. Catal*. 306: 116-128.

[3] Neofytidis, Ch., Dracopoulos, V., Neophytides, S.G. & Niakolas, D.K. (2018). *Catal. Tod.* 310: 157-165

[4] Pakhare, D. & Spivey, J. (2014). Chem. Soc. Rev. 43: 7813-7837.

[5] Niakolas, D.K., Neofytidis, Ch., Neophytides, S.G. (2017). *Frontiers in Environ. Science*. 5: 78